## Slide 1: Reference frames for EBSPs

## Slide 2: Microscope Orientations
Orientations in the SFEG and Helios are generally defined as shown
This orientation set up is defined as “Setting 2” in OIM DC and OIM Analysis
Euler angles are based off the axis A1, A2, and A3
A1, A2, and A3 change with the stage tilt only and are not related to the stage position or rotation
x, y, and z define a position on the sample but are not related to the Euler angles
RC, TD, and ND is a reference frame that can be assigned by the user to help him/her keep track of the sample orientation in the microscope

## Slide 3: EDAX Reference frames

## Slide 4
i
j
Imagesc used in OpenXY plots the same orientation as preview or other viewing tools – i.e. origin is in top left
Image(i,j)
x
y
Beam direction
The ‘1’ (RD) axis in the Euler angle frame is the ‘y’ sample axis, and the ‘2’ (TD) axis is the ‘x’ sample axis. Thus, in order to move from the Euler angle frame to the sample frame, we must flip x and y, and make z negative – i.e. multiply by:
If we are working in the sample frame (as defined by [x,y] obtained from the .ang file), then we must always adjust the Euler angles accordingly.
This is the camera view, i.e.
This is the ipf map
OIM reference frame setting 2?
Pattern center origin
PC is in units of phosphor / image size
PC
xstar
ystar
Notes: 150X Silicon Pats for Stu 1x1_r0c1
c is x and r is y in OIM

## Slide 5
x, y, and z coordinates
  Is used to describe the scan location on the sample
A1, A2, and A3 coordinates
  Is used to describe the orientation of the grains

## Slide 6: Alignment of Coordinate Systems
The rotation required to align the Oxford orientations with the EDAX orientations was found using MATLAB
An initial rotation of 90 degrees about the z axis on the Oxford orientations was required to align two company’s orientations
This means that if we rotate the EDAX coordinate system by -90 degrees about the z axis we will arrive at the Oxford coordinate system
EDAX
Oxford

## Slide 7: Reference Frames Used
 | Sample Frame (x and y positions of nodes/points) | Global Frame (basis for defining crystal frame using Euler angles, ϕ1φϕ2)
Simulations | Reference Frame 1 | Reference Frame 1
Oxford/Sandia Data (EBSD orientation data sent to OSU) | Reference Frame 2 | Reference Frame 1
EDAX/OpenXY (GND results) | Reference Frame 2 | Reference Frame 3

## Slide 8
i
j
Imagesc used in OpenXY plots the same orientation as preview or other viewing tools – i.e. origin is in top left
Image(i,j)
x
y
Beam direction
Notes: 150X Silicon Pats for Stu 1x1_r0c1
c is x and r is y in OIM

## Slide 9
Notes: 150X Silicon Pats for Stu 1x1_r0c33

## Slide 10
Notes: 150X Silicon Pats for Stu 1x1_r38c1

## Slide 11
Notes: scan1_x0y34.jpg
Silicon Scan 2018

## Slide 12
Notes: scan1_x1120y34.jpg

## Slide 13
Notes: scan1_x0y1247.jpg